## Slide 1: Resolution and Updates

## Slide 2: Updates:
Resolution calculations for r-CBGs.
Placed orders for needed parts(SLD, etc…).

## Slide 3: Resolution for r-CBGs
Grating ID: | Resolution: | Chirp Rate: | Focal Length:
SampleOne | 1.68nm | 1.14nm/mm | ~750mm
DC22E-003 | 0.45nm | .57 nm/mm | 1500mm
DC22E-001 | .3 nm | 0.298 nm/mm | 3m
r-CRBG-HE002 | .34nm | .374 nm/mm | 3m (1 Lens)
SampleXXX | 1.30nm | 1.69nm/mm | TBA
Calculation process: find FWHM and delta lambda using FWHM.
lambda
1064
1064
1064
1064
1064